| ORG.NO. 985227667 MVA / NORWAY | VISUAL TREATMENT GUIDELINE “COATSCALEREMOVER” / “CSR”+”CSR II” TREATMENT AND OPTIONS LINKED TO A VESSEL’S SEA WATER BALLAST TANKS AND VOID SPACE AS MAINTENANCE PROGRAM |
| --- | --- |
|  | Product applied | Condition | Step I | Curing | Condition | Step II | Curing | Step III | Condition | Life time |
| 1 | MULTI NOZZLE 5 –“HP” + “CSR” + “CSR II” | Ballast tank w/rust and scale due for removal | Apply CSR by spray or flotation | Time is dependent on temperature and ventilation | Scale is now detached from the steel and removed from tank by hand or mucking pump | Apply CSR II by spray or flotation onto FE-Oxide left on exposed surface | Time is dependent on temperature and ventilation |  | After curing, Sea Ballast Tank(s) have a long term protection. No hard coat required | Estimated 36 ++ months before touch up is required |
| 2 | MULTI NOZZLE 5 –“HP” + “CSR” + “CSR ” | Ballast tank w/rust and scale due for removal | Apply CSR by spray or flotation | Time is dependent on temperature and ventilation | Scale is now detached from the steel and removed from tank by hand or mucking pump | Apply CSR by spray or flotation onto FE-Oxide left on exposed surface | Time is dependent on temperature and ventilation |  | After curing, Sea Ballast Tank(s) have a temporarily protection | Estimated 18 ++ months before touch up is required |
| 3 | MULTI NOZZLE 5 –“HP” + “CSR” + “CSR” + “AQUATUFF HIGH FOAM” | Ballast tank w/rust and scale due for removal | Apply CSR by spray or flotation | Time is dependent on temperature and ventilation | Scale is now detached from the steel and removed from tank by hand or mucking pump | Apply CSR by spray or flotation onto FE-Oxide left on exposed surface | Time is dependent on temperature and ventilation | Aquatuff High Foam removes CSR & FE-Oxide. Rinse surface with fresh water! | Sea Ballast Tank(s) are prepared according to specification. Tolerant Epoxy Paint to be applied | Estimated 60 ++ months |
|  | “COATSCALEREMOVER” – “CSR” + “CSR II” ARE ENVIRONMENTALLY FRIENDLY & ISO 14001 CERTIFIED. OUR COMPANY WEBSITE www.trustper.com PROVIDES DETAILED INFORMATION AND DOCUMENTATION. WE ARE PLEASED TO RECEIVE ANY INQUIRIES TO OUR E-MAIL ADDRESS: per@trustper.com |