“Rust & Scale Substrate Specification Target by Grading”

EVALUATION PRIOR TO PROTECTIVE APPLICATION

(EXPLANATION TO NUMBERS RELATED TO GIVEN GRADE)

“RUST & SCALE (2Fe2O3) SUBSTRATE SPECIFICATION SETTINGS”

MAIN PURPOSE IS TO SIMPLIFY BALLAST TANK

REPORTING AND TANK STATUS, MAKING RECOMMENDATIONS.

ACKNOWLEDGMENT BY GRADE AND SPECIFICATION

10. GRADE  XXXL  ): Extreme substrate build up in multiple scale layers.

Removal: Major detachment by use of mechanical / electrolytic impact.

9. GRADE      XXL ):  Excessive substrate build up in multiple scale layers.

Removal: Major detachment by use of mechanical / electrolytic impact.

8. GRADE         XL ): Extensive substrate build up in multiple scale layers.

Removal: Major detachment by use of mechanical / electrolytic impact.

Scale layer detachment by use of highly penetrative liquid treatment.

7. GRADE            L ):  Significant substrate build up in multiple scale layers.

Removal: Scale layer detachment by use of highly penetrative and                          temporary steel protective treatment. Application by spray / floatation.

6. GRADE	M ):  Dense substrate build up in multiple scale layers.

Removal: Scale layer detachment by use of highly penetrative and   temporary steel protective treatment. Application by spray / floatation.

5. GRADE        MS ):. Highly dense substrate build up in multiple scale layers.

Removal: Scale layer detachment by use of highly penetrative and  temporary protective treatment. Application by spray / floatation.

4. GRADE	  S ): Strongly dense substrate build up in multiple scale layers.

Removal: Scale layer detachment by use of highly penetrative and  temporary protective treatment. Application by spray / floatation.

3. GRADE	XS ): Super dense scale substrate build up, layers not easily recognized.

Removal: Scale layer detachment by use of highly penetrative and temporary protective treatment. Application by spray / floatation.

2. GRADE        XXS ): Super firm substrate build up, measures made by instrumentation.

Removal: Scale layer detachment by use of highly penetrative and temporary protective treatment. Application by spray / floatation.

1. GRADE     XXXS ): Scale free surface on sound steel, which stays temporary protected.