ENVIRONMENTAL STATEMENT

FOR

“COATSCALEREMOVER REPMA®™”

PRODUCT – Hereinafter named “CSR” in following Environmental property description.

“CSR” is a blend of vegetable oils, driers, wetting agents and corrosion inhibitors. Its primary use is application as rust remover and temporary corrosion inhibitor in seawater ballast tanks, prior to achievable application of a more permanent protective hard coating.

“CSR” dries to a soft, non-sticky transparent coating when cured, better known as the “Fingertip-Touch” test. “CSR” has product property recognized as “Semi-hard Coating”.

“CSR” is safe both to the environment and the personnel handling it. “CSR” contains not any hydrocarbon solvents or oils, and all ingredients are completely biodegradable and environmental friendly.

“CSR” PHYSICAL PROPERTIES

Density at 20 ºC, g/l: 	  0,92

Appearance:		  Red, clear liquid. Becomes transparent, to light yellow after drying.

Viscosity at 20 °C, cSt:     55

Drying time (non-sticky): Approximately 12 hrs, to 2 days, depending on air-blower capacity for ventilation, the corrosion substrate, humidity and temperatures above or below 20 ºC.

Stability: 			  Infinite, when stored in closed container and stable after freezing.

Active content, %              Above 90

“CSR” HANDLING INSTRUCTIONS & MAJOR SAFETY SUMMARY

“CSR” is manufactured by Unitor Chemicals A/S, Norway Tel:47-3335 1500/Fax:47-3335 1440.

“CSR” composition/information on ingredients is available in our Safety Data Sheet.

“CSR” is NOT regarded as health hazard under current legislation.

“CSR” is unknown for any serious long term effect, repeated exposure could lead to dry skin.

“CSR” is classified NOT dangerous for the environment with reference to EU legislation.

“CSR” has no requirement for warning label.

“CSR” Technical data sheet and Safety data sheet is obtainable on request.

Kaohsiung, 1 April 2008.

Per Schaanning / MD / Trustper A/S

Contact Tel. 886 -7522 7661 / E-mail: per@trustper.com

Contact Mob. 47-9518 9116